EXPORTER DECLARATION

KSO SCISI VO No. : X.36.105839

| Importer Name | : | PT. PANDROL INDONESIA |
| --- | --- | --- |
| Invoice No. | : | 250304-PANDROL |
| Quantity | : | 2375 pcs |
| Weight | : | 1830kg (GW) |

We, hereby declare that the Goods exported are:

| Description of good | : | GS195 COACHSCREW C225/195 Ø25 Hexagon Head Type J - No. 13 Class 5.6 Hot Dip Galvanise GS195 COACHSCREW C225/195 Hexagonal Head Type J - No. 14 Class 5.6 GS195 COACHSCREW C225/195 Ø25 Hexagon Head Type J - No. 15 Class 5.6 Hot Dip Galvanise GS195 COACHSCREW C225/195 Hexagonal Head Type J - No. 16 Class 5.6 (HDG) Hot Dip Galvanised GS195 COACHSCREW C225/195 Ø25 Hexagon Head Type J - No. 17 Class 5.6 Hot Dip Galvanise |
| --- | --- | --- |
| Mill process *) | : | Hot Rolled |
| Size )* | : | 25X189, 25X194, 25X199, 25X204, 25X209 (size of product) |
| Standard *) | : | ISO898-1 |
| Grade *) | : | 5.6 |
| Coating | : | HDG |
| Coating weight | : |  |
| Application **) | : |  |
| Manufacturer *) | : | SUZHOU SUDELAN RAILWAY PARTS CO.,LTD. |
| Origin *) | : | CN |

| Chemical Composition (%) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C | Si | P | S | Mn | Ni | Cu | Cr | B | V | Mo | W | Al | Co | Pb | Se | Te | Bi |
| 0.35 | 0.14 | 0.015 | 0.002 | 0.71 |  |  |  |  |  |  |  |  |  |  |  |  |  |

Issued by The Exporter of above mention goods,

| Date of Issuance : | 2025-3-7 |
| --- | --- |
| Country of issuance : | CN |

| Full name : | Signature (Authorized) |  |
| --- | --- | --- |
| Title : |  |  |

*) Shall be filled in / stated

**) Shall be filled in / stated for Tube and Steel Derivatives Product