Pandrol Order Reference: PO001040

Date:2025-03-22

Certificate of Conformance

This is to confirm the component(s) described below comply with the applicable Pandrol specification and Pandrol drawing. The inspection and test results shown are taken from the manufactured batch(es) of product supplied on the order reference(s) shown above.

| Component | Quantity | Specification | Results |
| --- | --- | --- | --- |
| 923393 | 17000 | Composition Complies with a spring steel with UIC 864-3-0 | OK |
|  |  | Dimensions Complies with Pandrol drawing Pandrol drawing 923393 issue A3 22+1/-1mm | 21.5,21.8,22.0,22.4 |
|  |  | φ25+1.2/-0mm | 25.5,25.8,25.6,26.0 |
|  |  | 10+0.2/-0.2mm | 9.8,10.0,10.1,10.2 |
|  |  | 6+0.2/-0.2mm | 5.8,6.0,6.1,6.2 |
|  |  | Height difference of the horizontal plane 2~3mm | 2.1,2.2,2.2,2.3 |
|  |  | Deformation quantity ≤0.8mm | 0.6,0.6,0.7,0.7 |
|  |  | Appearance Free from harmful burrs Pandrol specification LW-L issue 1 | OK, OK, OK, OK |
|  |  | HDG ≥45μm | 60,71,86,95 |
|  |  | Elasticity H≥2/3 original H | 18.4,18.5,18.6,18.7 |
|  |  | Hardness HRC45-51 | 46,46,47,48 |
|  |  | rererse 90°noflaw | OK , OK, OK, OK |

Out of specification results are shown in red

Signed on behalf of component supplier’s QA Representative

__________________________

Signature