Pandrol Order Reference: F22333

Date:2022-06-27

Certificate of Conformance

This is to confirm the component(s) described below comply with the applicable Pandrol specification and Pandrol drawing. The inspection and test results shown are taken from the manufactured batch(es) of product supplied on the order reference(s) shown above.

| Component | Quantity | Specification | Results |
| --- | --- | --- | --- |
| 6164 | 12000 | Composition Complies with a spring steel wire grade to 5.6 with ISO 898-1 | OK |
|  |  | Dimensions Complies with Pandrol drawing Pandrol drawing 11212/1 issue A.2 172+5/-5mm | 168.9,169.2,169.5,170.3 |
|  |  | φ24+0.7/-0.3mm | 23.8,23.9,24.0,23.9 |
|  |  | 57+2/-2mm | 55.5,55.8,56.4,55.7 |
|  |  | Appearance Free from harmful burrs Pandrol specification LW-L issue 1 | OK, OK, OK, OK |
|  |  | HDG 50um to ISO 10684 | 69,78,86,89 |
|  |  | Tensile strength ≥500Mpa to UIC 864-1 | 606,613,,602,597 |
|  |  | Elongation ≥20% to UIC 864-1 | 23,22,23,23 |
|  |  | Bending test for 30 degree without crack to UIC 864-1 | OK , OK, OK, OK |

Out of specification results are shown in red

Signed on behalf of component supplier’s QA Representative

__________________________

Signature